# Battery Cycle Life Test

Summary report for the 18650 cell qualification programme

# 1. Purpose

This report summarises the cycle life results collected for the candidate 18650 lithium-ion cell across three charge rates. The programme's aim was to establish whether the cell retains at least 80 percent of its rated capacity after 500 full charge-discharge cycles, the threshold this product line requires before a supplier is qualified for volume orders.

# 2. Method

Twelve cells were drawn at random from a single production lot and divided into three groups of four, one group per charge rate: 0.5C, 1.0C and 1.5C. Each cell was cycled between 3.0V and 4.2V at 23C in a temperature-controlled chamber, with a full capacity check performed every 50 cycles on a calibrated cycler.

Cells that fell outside 2 percent of the group's mean capacity at the first check were flagged and continued on a separate log, so a single early outlier would not distort the reported group average.

Two cells were withdrawn from the programme before the 500-cycle mark: one for a connector fault unrelated to the cell itself, and one for a thermal excursion that exceeded the test's safety envelope. Neither withdrawal is included in the averages below.

# 3. Results

Table 1 lists the capacity retention measured at the 500-cycle checkpoint for each group, averaged across the surviving cells in that group.

| Charge rate | Cells | Capacity retention | Notes |
| --- | --- | --- | --- |
| 0.5C | 4 | 86.4% | Within spec |
| 1.0C | 3 | 83.1% | Within spec |
| 1.5C | 3 | 76.8% | Below 80% threshold |

The 1.5C group is the only one that falls short of the qualification threshold. Its degradation curve was noticeably steeper after cycle 300, which is consistent with accelerated lithium plating at the higher charge rate rather than a gradual, linear fade.

# 4. Observations

- Internal resistance rose by roughly 40 percent across all three groups over the course of the programme, with the steepest rise in the 1.5C group.

- No swelling or venting was observed on any cell at teardown.

- Capacity fade was closely linear for the 0.5C and 1.0C groups; the 1.5C group showed the knee described above.

# 5. Conclusion

The candidate cell meets the 80 percent retention threshold at both 0.5C and 1.0C charge rates but not at 1.5C. If the product's charging profile can be capped at 1.0C in the field, this cell is recommended for qualification. If 1.5C fast charging is a requirement, a different cell or a revised charge algorithm should be evaluated before this supplier is approved for that use case.

This has a footnote about test conditions

Ambient temperature held at 23C +/- 2C for the duration of the test programme.